## Slide 1: Unit 5 Non ferrous metal and alloys
Visit for more Learning Resources

## Slide 2: Co related to chapter
Select suitable non metals for particular applications as per properties.

## Slide 3: Copper and copper alloys
Properties of copper
1)it has good ductility and malleability because of its fcc structure.
2) It has high electrical and thermal conductivity.
3) It is non magnetic and has pleasing reddish color.
4)It has an ability of getting alloyed with many other metals which helps in improving its properties.
5)It has fairly good corrosion resistance to general atmospheric conditions.

## Slide 4: Application of Copper
It is widely used for electrical conductors, bus bars, automobile radiators, roofing, pressure vessels, kettles, utensils, coins and other application.
Copper containing about 0.3% arsenic is called arsenical copper and used for condenser, heat exchanger and similar application because of its improved corrosion resistance.
Copper containing about 0.6% tellurium is called free cutting copper because of its excellent machinability and it is used for bolts, studs, welding tips and electrical parts such as contact pins, switch gear, relay etc.

## Slide 5: Copper alloys
Brasses
Brasses are the alloys of copper and zinc.
Brasses are classified as follows
1)α –brasses
2)α-β brasses
3)Red brasses and yellow brasses.
α –brasses contain zinc less than 30% and α-β brasses
Contain zinc between 30 to 44%.
Below 20% zinc, color of brasses is red and above 20% zinc, the color is yellow.

## Slide 6: Copper alloys
α – brasses
Composition: Zinc less than 30%
Properties: Ductile, soft, malleable and fairly good corrosion resistance.
Application:
Cold rolling
Wire drawing
Press work.

## Slide 7: Copper alloys
Cap copper:
Composition: zinc between 2 to 5%.
If zinc is not added ,copper oxide present in the structure reduces ductility and malleability.
Properties: cap copper is very ductile.
Application: used as cap detonators in ammunition factories.
B)Gilding metal:
Composition: zinc from 5 to 15%.

## Slide 8: Copper alloys
Application: bullet envelopes, drawn containers, condenser tubes, coins, needles, emblems and dress jewelry because of color like gold.
c)Cartridge brass:
Composition: about 30% zinc.
Properties: maximum ductility and malleability amongst all the brasses.
Application: for forming by deep drawing, stretching, trimming, spinning and press work operations.
It is also used for cartridge cases, radiator fins, lamp fixture, rivets and springs.

## Slide 9: Copper alloys
D) Admiralty brass:
Composition: about 1% tin is added to cartridge brass to improve the corrosion resistance and such a brass is called as admiralty brass.
22% Zn, 2% Al and about 0.04% As.
Application: condenser tubes and heat exchanger in steam power plant.
Marine application.

## Slide 10: Copper alloys
α-β brasses:
Composition: zinc between 32 to 40%
Properties: hard, strong and are fabricated by hot working processes , more ductile and malleable, cheap, poor corrosion resistance.
Muntz metal
Composition: 40% zinc with balance copper.
Properties: this becomes single phase at about 700c.
It can be readily hot worked , extruded or rolled in temp. range of 600 to 800c.

## Slide 11: Copper alloys
Tensile strength of 35 to 40% kg/mm2.
Hardness of 100 to 120 v.p.n.
Application: utensils, shaft, nuts and bolts, pump parts, condenser tubes .
B) Naval brass:
Composition: 1% tin to Muntz metal increases corrosion resistance to marine environment and brass is called as naval brass or Tobin bronze.
Application: marine hardware, propeller shaft, piston rods, nuts and bolts and welding rods.

## Slide 12: Copper alloys
c)Leaded brass:
composition: lead is added in small amount (1 to 3%) to improve machinability of brasses.
Properties: addition of lead is done to both the muntz metal and naval brass for improvement of machinability.
This results in slight decrease in ductility and impact strength of the alloys.
D) High tensile brasses:
Composition: Alloying elements such as Al, Fe, Mn, Sn and Ni are added to 60-40 brass(Muntz metal) to increase its tensile strength.

## Slide 13: Copper alloys
Brass containing two or more above element is called as high tensile brasses.
One of its manganese bronze containing up to 1% Mn, 2% Fe, 39% Zn and balance copper.
It has good sea water resistance, tensile strength of 40-55 kg/mm2 and elongation of 20 to 30%..
Application: marine engine pumps, ship propellers, gears, valve bodies..
E)Brazing brass:
Composition: brass with 50-50 composition is used for brazing purpose. Property: brittle.

## Slide 14: Bronze
Bronze are the alloys of copper containing elements other than zinc.
In these alloys , zinc may be present in small amount.
Originally the name bronze was used to denote copper-tin alloys.
Commercially important bronzes are aluminum bronzes, tin bronzes, beryllium bronzes and silicon bronzes.

## Slide 15: Aluminium Bronze
Composition: copper + aluminum
Commercial aluminium bronzes contain 4 to 11% aluminium.
Other elements such as Fe, Ni, Mn and Si may be added too these bronzes for improvement of certain properties.
Properties:
Good strength, ductility, toughness.
Good bearing properties.
Good corrosion resistance.
Good fatigue resistance.
Applications: jewelry, cigarette cases, heat exchangers, chemical plants, pump castings, valve fittings, propellers, cylinder heads, gears, dies, bearings, spark plug bodies and electrical contacts.

## Slide 16: Tin Bronze
Composition: tin + copper
Classification:
A)Alloy up to 8% tin:
Good ductility, malleability, good corrosion resistance.
They can be easily cold worked and hence are used in the form of sheets, wires and coins.
B)Alloy between 8 to 12 % tin:
Used for pumps, gears, heavy load bearings and marine fittings to resists sea water corrosion.
c)Alloy between 12 to 20% tin:
They are mainly used for bearings.

## Slide 17: Tin Bronze
D)Alloy between 20 to 25% tin:
They are principally used for bells and are called as bell metal.
Very hard and brittle, and give ringing sound.
Gun metal:
It contain about 10 % tin and 2% zinc.
It is widely used for gun barrels and ordnance parts, marine castings, gears, bearings, valve bodies and similar applications.

## Slide 18: Beryllium bronze
Solubility of beryllium in copper is 2.1 % at 864c and decreases with decreasing temp.
Properties:
Tensile strength 130 to 140 kg/mm2
Hardness 350 BHN
Good corrosion resistance, good fatigue resistance, high resilience and good bearing properties
Low elastic hysteresis and non sparking characteristics.
Application : springs, diaphragms, flexible bellows, gears, bearing and certain tool like hammers.
Also used for electrical contacts and moulds for forming of plastics.

## Slide 19: silicon bronze
The alloy of silicon and copper is called as silicon bronze.
Properties:
High resistance to corrosion,
High tensile strength,
Cold working, hot working, casting, good machinability
High toughness.
Application :
High strength bolts, rivets, springs, propeller shafts and bells.
They are produced in the form of strips, plates, wires, rods, tubes, pipes, and castings.

## Slide 20: Copper nickel alloys
Properties:
Ductile, malleable and can be worked both in cold and hot conditions.
The corrosion resistance increases with increase in nickel.
Tensile strength, fatigue strength increases with nickel.
Application : It is used as resistor .
Used for thermocouple wires, locomotive fire boxes as stay rods,
Marine condensers, turbine blades, bullet envelopes and coins, resistance wire, valve parts, pump rod liners, impellers and part in chemical industry, rivets, screws, table flatware, costume jewelry, name plates, radio dials, camera and optical parts.

## Slide 21: Aluminium and aluminium alloys
Properties:
It is ductile and malleable due to fcc structure.
It is light in weight.
Good thermal and electrical conductivity,
It has excellent corrosion and oxidation resistance.
Corrosion product of aluminium is non toxic .
It remains ductile and tough up to -40 c.
Non magnetic, non sparking in character.
It has excellent ability of getting alloyed with other elements.
Application :
Cooking utensils, combs, collar buttons, toasters, mixers,

## Slide 22: Aluminium and aluminium alloys
electrical conductors, food containers, paint, name plates, ash trays, flower pots, coins , bicycles, motorcycles, trucks, and buses, aero planes, and marine vessels.

## Slide 23: Y-alloys(LM 14)
Composition:
This is high strength aluminium alloy and contains about 4% copper, 2% nickel and 1.5% magnesium.
Properties:
It has excellent ability to retain the strength at elevated temp. with fairly good corrosion resistance.
It can be easily cast and rolled, but it is chiefly used in the cast form.
Application:
It is mainly used for pistons and cylinders heads of diesel and high duty petrol engines.

## Slide 24: Hinduminium (RR 350)
Composition:
5% Cu and 1.5 % Ni with small amount of Mn, Ti, Sb, Co and Zr.
Property: creep resistance
Application: aero engine.
Duralumin:
4.5% Cu+ magnesium(0.5%) +manganese (about 0.5%) .
Good strength
Shock resistance
Corrosion resistance
Application : air craft castings.

## Slide 25: Bearing materials
properties:
The friction between the bearing and the rotating shaft should be minimum.
It should be hard and wear resistance and longer life.
It should have sufficient load bearing ability.
It should have sufficient plasticity.
It should have high fatigue resistance
It should have good thermal conductivity.
It should have very low or very high melting point
It should have oil retaining capacity
Good corrosion resistance, cheap, readily available.

## Slide 26: Bearing materials
White metal ( Babbitts ):
Babbitts are either lead based or tin based alloys.
Pb based: 1-10% Sn, Pb- balance, 10-15%Sb, 1.5-3.5%Cu,( others 1.25-1.75%Cd, as0-1%)
Sn based: Sn balance, Pb up to 10%, Sb 5-12%, Cu 3-5%(others As: 0-0.1%)
properties:
corrosion resistance, Wear resistance, Costly
Lead is added to theses Babbitts to reduce their cost.
Application: lorry diesel engine crank shafts.

## Slide 27: Bearing materials
Copper lead alloy
Copper lead bearings are widely used in automotive and aeronautic applications.
These alloy contain lead in the range of 20 to 40 % with small amount of tin.
Other bearing materials
Silver bearing
Tin bronze
Aluminium alloys
Gray cast iron

## Slide 28: Porous self lubricating bearing.
These bearings are manufactured by powder metallurgy.
Porous bearings are made from copper or iron base powders with as much as 40 to 50 % porosity.
And are impregnated with oil.
During the use , oil from the pores slowly comes out and forms a lubricating film on the moving surface.
When working is stopped , the oil goes back to the pores by capillary action.
They do not require any external lubrication and hence called as self lubricating bearings.
Cu(90%) Sn(10%) graphite and Fe(96%) bearing are widely used as self lubricating bearing.
For more detail contact us